## Slide 1: Low-Dimensional Nanoelectronic Materials Use-Case Group
Mark Hersam, NU
Lincoln Lauhon, NU
Albert Davydov, NIST
Francesca Tavazza, NIST
Arunima Singh, NIST

## Slide 2: Use-Case Group Overview and Design Goals
Vision Statement: Understand and realize p-type and n-type doping in the low-dimensional limit
Functions: rectification, light emission, photoresponse, photovoltaic
Design goals:
  Control doping and carrier concentration in the low-dimensional limit
  Realize heterostructures from low-dimensional nanoelectronic materials
Experimental methods:
  Charge transport (automated wafer prober)
  Optical spectroscopy (e.g., PL, Raman)
  Scanning probe methods
  Atom probe tomography
Computational methods:
  Multi-scale modeling
  Molecular dynamics, DFT
  Finite element methods

## Slide 3: Use-Case Group System Design Chart
PROCESSING
STRUCTURE
PROPERTIES
PERFORMANCE
Optoelectronics
Transistor
Memristor
Luminescence
Air Stability
Charge Transport
Carrier type
Carrier concentration
Carrier mobility
Band Gap
Defect Migration
Microstructure
Grain boundaries
Grain size
Grain orientation
Thickness
Annealing
Etching
Chemical Functionalization
Regrowth
Encapsulation
CVD
CVT
ALD
Substrate
Growth Method
Composition:
Stoichiometry
Doping

## Slide 4: Design Sub-Goal: Substitutional Doping
PROCESSING
STRUCTURE
PROPERTIES
PERFORMANCE
Transistor
Charge Transport
Carrier type
Carrier concentration
Carrier mobility
Band Gap
Composition:
Stoichiometry
Doping
Growth Method:
Chemical Vapor Transport
Chemical Vapor Transport
Atom Probe Tomography
Density Functional Theory
NIST: Singh, Tavazza, Davydov
NU: Ren, Lauhon

## Slide 5: Y2 Accomplishments: Atom Probe and DFT of Substitutional Doping
Accomplishments:
Demonstrated dopant analysis in 2-D materials by atom probe tomography for the first time.
Resolved the distribution of substitutional dopants between chemically distinct sites.
Employed density functional theory calculations to understand preferred doping configurations.

## Slide 6: Atom Probe Tomography of (PbSe)5(Bi2Se3)3
PbSe
Bi2Se3
1.65 nm
Samples grown by Kanatzidis Group @NU
Ag
Se
Bi
Pb
10 nm
10 nm
10 nm
10 nm
Ag doping changes material from metal to superconductor, providing an approach to engineer novel heterojunctions.
Ag is expected to dope only the PbSe layer. Can dopant location be resolved by APT?

## Slide 7: Ag Dopes Both the Pb and Bi layers
1.65 nm
PbSe
Bi2Se3
Ag in Pb-Se layer
Spatial Distribution Map
Ag in Bi-Se layer
SDM identifies location of Ag dopant atoms relative to Bi, Pb.
Composition profile gives the dopant concentration in each layer.

## Slide 8
Ag-Ag pairs have lowest defect formation energy.
# configurations + low energy  highest probability.
DFT Calculation of Favorable Ag Configurations
  66 configurations
  44 configurations
  120 configurations

## Slide 9: DFT Calculation of Favorable Ag Configurations
DFT calculation confirms that Ag doping in both layers is energetically favorable.
Significance: Demonstrated capability to predict and measure substitutional dopant locations in 2D materials.
RDF from APT provides evidence of the Ag-Ag pairing/clusters.
Defect Formation Energies
Radial Distribution Function

## Slide 10: Design Sub-Goal: Chemical Functionalization Doping
PROCESSING
STRUCTURE
PROPERTIES
PERFORMANCE
Transistor
Air Stability
Charge Transport
Carrier type
Carrier concentration
Carrier mobility
Chemical Functionalization
Composition:
Stoichiometry
Doping
Chemical Functionalization
Doping of Two-Dimensional
Black Phosphorus:

## Slide 11: Y2 Accomplishments: Diazonium Functionalization of Black Phosphorus
Accomplishments:
First covalent modification of 2D black phosphorus has been achieved with diazonium chemistry.
Ambient stability of 2D black phosphorus is significantly improved following functionalization.
Functionalization leads to controlled p-type doping and improved transistor metrics (e.g., mobility and on/off ratio).
M. C. Hersam, T. J. Marks, et al., Nature Chemistry, in press, 2016.

## Slide 12: DFT Predicts Stable Arylation of Black Phosphorus
DFT predicts stable covalent bonding of diazonium aryl radical intermediates to black phosphorus
M. C. Hersam, T. J. Marks, et al., Nature Chemistry, in press, 2016.

## Slide 13: Experimental Confirmation of Arylation of Black Phosphorus
M. C. Hersam, T. J. Marks, et al., Nature Chemistry, in press, 2016.
Atomic force microscopy shows an increase in black phosphorus flake height consistent with arylation
(corroborated by XPS and Raman)
2 μm
2 μm

## Slide 14: Chemical Functionalization Improves the Ambient Stability of Two-Dimensional Black Phosphorus
M. C. Hersam, T. J. Marks, et al., Nature Chemistry, in press, 2016.
With covalent
functionalization:
Without covalent
functionalization:
0 days
10 days
0 days
10 days
2 μm
2 μm
2 μm
2 μm
Chemical functionalization achieves the design goal of improving the ambient stability of 2D black phosphorus

## Slide 15: Chemical Functionalization Leads to Controlled p-type Doping and Improved Device Metrics
M. C. Hersam, T. J. Marks, et al., Nature Chemistry, in press, 2016.
Covalent functionalization leads to controlled p-type doping as evidence by rightward shift in transistor transfer curves.
Transistor metrics (e.g., mobility and on/off ratio) are optimized at intermediate functionalization conditions.

## Slide 16: Design Sub-Goal: Growth of Nanoelectronic Heterostructures
PROCESSING
STRUCTURE
PROPERTIES
PERFORMANCE
Memristor
Defect Migration
Chemical Vapor Deposition
Substrate
Growth Method
MoS2/Graphene
Heterostructures:
Microstructure
Grain boundaries
Grain size
Grain orientation

## Slide 17: Y2 Accomplishments: MoS2/Graphene Heterostructures
Accomplishments:
Rotationally commensurate growth of MoS2 on epitaxial graphene on SiC by chemical vapor deposition.
CVD MoS2 on epi-graphene shows higher hole doping and reduced strain compared to CVD MoS2 on SiO2.
Rotational commensurability implies only 2 possible angles (30° and 60°) for CVD MoS2 grain boundaries on epi-graphene.
M. C. Hersam, M. J. Bedzyk, et al., ACS Nano, 10, 1067 (2016).

## Slide 18: CVD Growth of MoS2 on Epi-Graphene on SiC
M. C. Hersam, M. J. Bedzyk, et al., ACS Nano, 10, 1067 (2016).
Chemical vapor deposition growth of MoS2 on epitaxial graphene on SiC leads to most MoS2 flakes being rotationally aligned or 30° misaligned

## Slide 19: Raman Analysis of CVD MoS2 on Epi-Graphene
M. C. Hersam, M. J. Bedzyk, et al., ACS Nano, 10, 1067 (2016).
Raman analysis shows that CVD MoS2 on epi-graphene possesses higher hole doping and reduced strain compared to CVD MoS2 on SiO2

## Slide 20: Electronic Structure of CVD MoS2 on Epi-Graphene
M. C. Hersam, M. J. Bedzyk, et al., ACS Nano, 10, 1067 (2016).
Scanning tunneling spectroscopy reveals strong contrast between zero bandgap epi-graphene and the ~2 eV bandgap of single-layer MoS2

## Slide 21: GIWAXS of CVD MoS2 on Epi-Graphene
M. C. Hersam, M. J. Bedzyk, et al., ACS Nano, 10, 1067 (2016).
86 % 14 %
Synchrotron grazing-incidence wide-angle X-ray scattering (GIWAXS) reveals rotational commensurability between CVD MoS2 and epi-graphene

## Slide 22: NIST Collaboration: Multi-Scale Modeling of 2D Material Growth and Heterostructures
  Developed DFT framework and python-based tool to automate high-throughput screening of substrates for synthesis and functionalization of 2D materials
  In-progress: Integrating with phase-field models for bottom-up design of 2D materials with controllable structural, mechanical and electronic properties
NIST: Singh, Tavazza

## Slide 23: NIST Collaboration: Modeling of Alloy Phase Diagrams for Band-Gap Engineering
Case 1: Alloying on Chalcogen sublattice - MoS2(1-x)Te2x
Case 2: Alloying on Metal sublattice - Nb(1-x)WxSe2
Nb is а p-type dopant
(1) Calculate DFT formation energies
HCE = E(s1…sn) = S{i,j}Jijsisj + S{i,j,k}Jijksisjsk + …
HCE=SaJasa
(2) Fit Cluster Expansion Hamiltonian:
(3) Calculate phase diagrams (via MC simulation):
МоТе2
МоS2
NIST: Singh, Tavazza

## Slide 24: NIST Collaboration: Benchmarked Library of Two-Dimensional Nanomaterials
CVT single crystal growth:
  2D Library for developing controlled doping (computational + experim. database)
  NbSe2; MoTe2; Mo1-xWxTe2, WS2(1-x)Te2x, GaSe
CVD wafer-scale growth:
  Metal sulfurization: Mo + S2  MoS2
  Chloride-chemistry CVD: MoCl5 + H2S  MoS2 (Year 3)
  Pulsed MOCVD/ALD: EDNOMo + DEDS  MoS2
Low-temperature solution growth (to complement NU’s graphene inks)
  “MoS2” ink  anneal  3D printing of MoS2/graphene devices
NIST: Davydov, Krylyuk, Maslar, Debnath

## Slide 25: NIST Collaboration: 2D Semiconductor/Metal Phase Change
NIST-grown 2D MoTe2 layers show semiconductor/metal phase transition
NU + NIST device fabrication and testing to understand charge transport
2H
1T’
Raman Spectra
Phase Diagram
Transistor Transfer Curves
NIST: Davydov, Krylyuk, Sharma
NU: Hersam, Beck, Bergeron

## Slide 26: Industrial Collaborations
Three graphene inks (inkjet, gravure, and screen printable) are being distributed by Sigma
Black phosphorus inks have been delivered to IBM T. J. Watson Research Center (Mathias Steiner, Michael Engel) for device testing

## Slide 27: Future Work: Substitutional Doping
Work at NIST on growth and processing of S-doped WTe2 for metal-semiconductor junctions. X. Ren (NU student) will visit NIST.
Develop sample preparation methods to facilitate atom probe analysis of transition metal dichalcogenides (TMDs).
With NIST, correlate dopant/alloying in TMDs and electrical properties both experimentally (APT) and from first principles (DFT).

## Slide 28: Future Work: Chemical Functionalization Doping
Explore variable temperature charge transport in black phosphorus vertical field-effect transistors.
Perform 1/f noise characterization of black phosphorus transistors (initial devices sent to NIST).
Elaborate chemical functionalization doping to other nanoelectronic materials (e.g., transition metal dichalcogenides and IV-VI compounds).

## Slide 29: Future Work: Growth of Nanoelectronic Heterostructures
Explore grain boundary physical and electronic structure for rotationally commensurate MoS2/graphene heterojunctions.
Develop seeded growth methods to control the position and orientation of grain boundaries.
Study the effect of engineered grain boundaries on charge transport (e.g., memristors).