## Slide 1: Soft Matter Design Based On Charge Complexation
Matthew Tirrell
University of Chicago
Argonne National Laboratory

## Slide 2
Multivalent electrostatic interactions are an effective and underexploited tool in molecular self-assembly, e.g., to make hydrogels with tunable moduli and other desirable characteristics of biomaterials.
Easy incorporation of particles to make composites
Design goals for biomaterials
  Tune the modulus to match tissue of interest
  Self-healing is helpful for cell migration and injectability
  Add biofunctionality where needed
  How we determine bulk properties of biomaterials from macromolecular size and charge?
Polymer charge complexation applied to biomaterials

## Slide 3
Polyelectrolyte complexes (PECs) form when oppositely charged
polyelectrolytes are mixed in aqueous solution (electrostatic interactions)
Srivastava & Tirrell, Advances in Chemical Physics, 2016
Protective shell
from excreted proteins
Marine organisms
Membrane-less
compartments
Stable particle dispersions
Polyanion solution
Polycation solution
Polyelectrolyte complex (PEC)
Polyelectrolyte Complexation

## Slide 4
Plys
PGlu
PEG-b-PLys
Plys-b-PEG-b-PLys
PAA
PAH
fPAGE
fPAGE-b-PEG
fPAGE-b-PEG-b-fPAGE
PDMAEMA
100 nm
Bulk Complexes
Complex-core Micelles
Crosslinked Hydrogels
Drug Delivery, Tissue Engineering, Encapsulation, Multi-Responsive Materials, Adhesives
Designer Polymers
Controllable Assembly
Polyelectrolytes
Platform for ‘Soft’ Material Design
Versatile Materials
PEC micelles & hydrogels
PEC stabilized biocomposites
Membrane-less compartments
Developing theoretical and computational underpinning for design
Range of
Applications
Notes: Key Advantages
Self-assembled hybrid materials
Aqueous environment
Easily tunable interactions
Designer properties

## Slide 5
PEC Phase Diagram
Driving forces
Electrostatic interactions between the polyelectrolyte chains
Release of counter ions associated with the polyelectrolyte chains
N = 200
N = 400
Binodal phase behavior predicted by Voorn-Overbeek mean field model
Combination of various experimental techniques
Meticulous investigation with an emphasis on:
  Salt partitioning in two phases
  Slope of the tie-lines
Experiments
Lines are guides to the eye
Coarse-Grained MD Simulations
Bead-spring chain with soft Coulomb for short range and Ewald Sum for long range interactions
Comparison with experiments (filled symbols) with varying chain lengths
Experimental data from Spruijt et al., Macromolecules, 2010
Li, Srivastava, Tirrell
Andreev, de Pablo

## Slide 7: Rheology: Salt-Frequency Superposition
Priftis and Tirrell
sec

## Slide 8: Rheology: Salt-Frequency Superposition
Andreev, de Pablo
Spruit, et al
MD anticipates the existence of
salt-frequency superposition
but theoretical understanding
of shift factors is still needed.

## Slide 9
Electrostatics Induced Solvent Selectivity
Charged Polymer
Neutral Polymer
Charged polymer-rich
Neutral polymer-rich
Strength of electrostatic interactions
can induce selectivity in a non-selective, neutral solvent
  At low , ion entropy drives solvent into the charged block
  At high , ionic correlations drive solvent into the neutral block
Solvent adsorption increases with
Can be extended to study micro-phase separation in charged-neutral block copolymers
Blends of charged and neutral polymers
Olvera de la Cruz
polymer phase
polymer phase

## Slide 10
Electrostatics Induced Solvent Selectivity
Charged Polymer
Neutral Polymer
Charged polymer-rich
Neutral polymer-rich
Strength of electrostatic interactions
can induce selectivity in a non-selective, neutral solvent
  At low , ion entropy drives solvent into the charged block
  At high , ionic correlations drive solvent into the neutral block
Solvent adsorption increases with
Can be extended to study micro-phase separation in charged-neutral block copolymers
Blends of charged and neutral polymers
Olvera de la Cruz
?

## Slide 11
Microphase Separation
Polyelectrolyte Complex Micelles
Micelles with hydrophilic cores
Complexation drives microphase separation
Cores can either be solid or liquid complexes
Excellent for drug and nucleic acid delivery

## Slide 12
Coarse-Grained Model for PEC Micelles
Diblock PEG polylysine + miRNA micelles
Large interfacial regions observed in density profiles
Contribute to better design and enhanced delivery efficiency
Andreev, de Pablo

## Slide 13: Lesion reduction by miR-92a inhibitor in complex with endothelium-targeted micelles
PBS
Naked
miR-92a inhibitor
Micelle/
inhibitor Ctl
Micelle/
miR-92a inhibitor

## Slide 14
Krogstad, D. V. et al. Macromolecules 2013, 46, 1512
Hunt, J. N. et. al., Adv. Mater. 2011, 23, 2327
Hydrophilic cores
Excellent encapsulation
propensities
Tunable chemistry & properties
Drug Delivery and
Tissue Growth Platforms
PEC Hydrogels: Self-Assembled Hybrids

## Slide 15
Triblocks
Diblocks
50%
40%
5%
Configurational entropy of micelles in the solution vs. conformational entropy of the neutral chain
Diblock copolymers are useful for individual micelles, triblock copolymers are useful for tough gels
P(AGE26-EO455-AGE26)
Guan.
P(AGE26-EO455-AGE26)
Sulf.
P(EO227-AGE26)
Guan.
P(EO227-AGE26)
Sulf.
Triblocks
Diblocks
Triblocks
Diblocks
2%
1%
2%
1%
PEG455 Midblock
PEG227 Midblock
(larger charged fraction)
vs.
Low Concentration Structures
Spherical Micelles vs. Connected Clusters
Srivastava, Tirrell

## Slide 16
No plateau at low q large clusters > 100 nm
Low q slope fractal dimension of clusters
Correlation peak position is independent of conc. Conc. independent PEC domain spacing
Correlation peak intensity increases with increasing conc. Domain number density increases with conc.
P(AGE26-EO455-AGE26), Guan. + Sulf.
P(AGE51-EO455-AGE51), Guan. + Sulf.
Triblock Copolymers Form Clusters
-1
-2
-2
-3
Low conc.
Wei, Prabhu
Srivastava, Tirrell

## Slide 17
Dynamic light scattering: multiple modes
C0.47
Micelle
Slow cluster-mode
Fast cooperative
mode
T = 25 C
Micelles, clusters & cooperative modes
PAGE26-PEG455-PAGE26
C = 15 wt%
PAGE26-PEG455-PAGE26
Multiple Relaxation Modes
Multiple modes of relaxation corresponding to various relaxation processes in clusters
PEC Core: Scattering (Rg = 13 nm) consistent with a diffusive mode by DLS (RH = 15.3 nm)
Cluster concentration-independent diffusion coefficient Dt of the slow mode
Correlation length within cluster exhibits diffusive dynamics Dcoop ~ C0.47 similar to neutral semidilute polymer solution predictions
Low conc.
Wei, Prabhu
Srivastava, Tirrell

## Slide 18
P(AGE60-EO455-AGE60)
Guan.
P(AGE60-EO455-AGE60)
Sulf.
Hydrogels: PEC Domain Arrangements
Srivastava, Tirrell

## Slide 19
Coarse-Grained Model for PEC Micelles
SAXS Investigations
Increasing
Charged Block
Length
PAGE15-PEO455-PAGE15
PAGE30-PEO455-PAGE30
PAGE60-PEO455-PAGE60
PAGE51-PEO455-PAGE51
PAGE26-PEO455-PAGE26
Srivastava, Tirrell

## Slide 20
Hydrogel Morphology Phase Diagram
Design of Tunable Gels
Charged:neutral block ratio length determines packing morphology
Qualitatively similar phase diagrams as predicted by theory
Phase diagrams are not superimposable: mid-block effects are not trivial
PEO227 midblock
Guan.
Sulf.
PEO455 midblock
Guan.
Sulf.
End-block fr.
Conc.
SCFT-EF calculations
Audus, Fredrickson et al., Soft Matter 2015
Srivastava, Tirrell

## Slide 21
Versatile Materials Built via Electrostatic Self-Assembly
PEC micelles and hydrogels
PEC stabilized biocomposites
Membrane-less compartments
Developing theoretical and computational underpinning for design
Drug Delivery, Tissue Engineering, Encapsulation, Multi-Responsive Materials, Adhesives
International Symposium on Multivalent Interactions in Polyelectrolytes: New Physics, Biology and Materials. Sponsored by CHiMaD and IME. University of Chicago, October 2-4, 2015. Co-Organizers: Juan de Pablo, Sheng Lin-Gibson, Vivek Prabhu, Monica Olvera de la Cruz, Matthew Tirrell
Conclusions

## Slide 22: Polyelectrolyte effects on CaP structure

## Slide 23
Polyelectrolyte effects on CaP structure

## Slide 24: Electric double layer of anisotropic dielectric colloids under electric fields
M. Han, H. Wu and E. Luijten
Eur. Phys. J., submitted
Field-directed assembly of patchy colloids gives a broad range of biomimetic patterns, from microtubes to double helices
The aggregation is driven by induced dipole moments, which arise from an interplay between dielectric effects and the EDL
Our newly developed method now makes it possible to solve this problem in simulations for colloids in both DC and AC fields
We use our findings to make experimentally important predictions on the role of field strength and frequency and on the preferred orientations for various particles
This work opens pathways toward predictive capabilities for polarizable building blocks for the field-directed assembly of new biomimetic materials
Notes: Anisotropic colloidal particles constitute an important class of building blocks for self-assembly directed by electrical fields. The aggregation of these building blocks is driven by induced dipole moments, which arise from an interplay between dielectric effects and the electric double layer. For particles that are anisotropic in shape, charge distribution, and dielectric properties, calculation of the electric double layer requires coupling of the ionic dynamics to a Poisson solver. We apply recently proposed methods to solve this problem for experimentally employed colloids in static and time-dependent electric fields. This allows us to predict the effects of field strength and frequency on the colloidal properties.